Fig. 1. Weight gain comparison between two micromonoliths before calcination

Fig. 2. XRD patterns for (A) RuAl and S-RuAl (calcined and reduced) and (B) micromonolithic devices (bare, pretreated M and coated M-RuAl). (*) RuO2; () -alumina; (Ru) metallic Ru; (o) martensite steel; (+) -Al2O3; (=) aluminium yttrium oxide

Fig. 3. TEM micrographs for reduced powder samples (A) RuAl and (B) S-RuAl

Fig. 4. N2 adsorption–desorption isotherms obtained for RuAl, S-RuAl and M-RuAl

| A |  |
| --- | --- |

| B RuAl -Al2O3 | -Al2O3 RuAl |
| --- | --- |
| Fig. 5. SEM micrographs of M-RuAl sample; (A) top and (B) cross section views |  |

| RuAl Resin -Al2O3 Fecralloy | Al |
| --- | --- |
| O | Ru |
| Fe | Cr |

Fig. 6. Mapping of cross section of M-RuAl

Fig. 7. In-line cross section in-depth compositional EDX analyses for M-RuAl from Fig. 6

Fig. 8. TPR profile for RuAl and S-RuAl

Fig. 9 (A) CO (solid lines) and CO2 (dash lines) conversions during S-MET with powders and micromonolithic catalysts. The selective temperature range, where less than 20 ppm CO is emitted with a total H2 consumption lower than 4% is also shown. (B) Selectivity towards CO methanation vs CO conversions. Feed composition: 0.03%CO, 15% CO2, 50%H2 (balance N2); WHSV: 80000 ml.g-1.min-1

Table 1

Textural properties of studied samples

| Code | SBET (m2 g-1) | Pore volume (cm3 g-1) | Pore size (nm) |
| --- | --- | --- | --- |
| RuAl | 149 | 0.36 | 6.0 |
| S-RuAl | 153 | 0.38 | 7.5 |
| M-RuAl | 154* | 0.37 | 7.0 |
| Al2O3 Nyacol** | 192 | 0.37 | 7.8 |

* Calculated from the amount of catalysts deposited

** Nyacol AL20 dried and calcined at 400°C 2h